Supplementary Information

Cross-dimensional machine learning of in-plane dielectric constants in two-dimensional materials from three-dimensional van der Waals crystals

This Supplementary Information consolidates the materials cited collectively in the main manuscript. It contains the definitions and mathematical expressions of the physically reconstructed descriptors, the Pearson-correlation analysis for representative descriptors, and the abbreviation map for the feature names used in the feature-ranking and distribution analyses.

Supplementary Table S1| Physically reconstructed features and mathematical expressions

The physically reconstructed descriptors below were introduced to express the geometry and response-relevant density of layered crystals and monolayers on a common effective-thickness basis. Roman text is used for descriptor labels and non-variable subscripts, whereas mathematical variables are italicized.

| Feature name | Symbol | Mathematical definition | Physical meaning |
| --- | --- | --- | --- |
| Effective thickness | teff | teff=zmax−zmin+rtopvdW+rbotvdW | Intrinsic layer thickness after removing the artificial vacuum contribution and adding the Bondi van der Waals radii of the two boundary atoms. |
| In-plane area | A2D | A2D=absinγ | Projected area of the two-dimensional unit cell in the xy plane. |
| Effective volume | Veff | Veff=A2D teff | Vacuum-independent three-dimensional volume intrinsically occupied by the material. |
| Effective density | ρeff | ρeff=McellVeff×1.660539 | Mass density distributed within the effective volume, expressed in g⋅cm−3. |
| Per-atom effective volume | veff | veff=Veff/Natoms | Average effective space assigned to each atom. |
| Structural dimensionality ratio | SDR | SDR=teffa+b | Geometric anisotropy measure for a two-dimensional layered structure. |
| Area-thickness ratio | AI | AI=A2Dteff | Relative proportion between in-plane extension and out-of-plane confinement. |
| van der Waals packing fraction | ϕEPF | ϕEPF=i=1N43πrivdW3Veff | Fraction of the effective volume occupied by atomic van der Waals hard spheres. |
| Polarizable volume factor | αEAP | αEAP=i=1NrivdW3Veff | Structural weighting factor positively correlated with macroscopic electronic polarizability. |
| Interfacial bonding strength | IBS | IBS=ρeffteff | Mass packing density per unit thickness, associated with intralayer chemical-bond strength. |
| Effective dielectric volume | VEDV | VEDV=Veff fNM | Polarization-response volume dominated by nonmetal atoms, where fNM is the nonmetal atomic fraction. |
| Maximum electronegativity difference | Δχmax | Δχmax=max{χi}−min{χi} | Range of Pauling electronegativities among elements in the unit cell, indicating the tendency toward ionicity. |
| Average bond length | ⟨d⟩ | ⟨d⟩=1Nbj=1Nbdj | Mean nearest-neighbor bond length determined using the CrystalNN criterion. |
| Bond-length standard deviation | σd | σd=1Nb−1j=1Nbdj−⟨d⟩2 | Structural disorder of the local coordination environment. |
| Centrosymmetry | Scentro | Scentro∈{0,1} | Whether the space group contains an inversion center; 1 denotes yes and 0 denotes no. |
| Asymmetric electronegativity index | Jχ | Jχ=χtop−χbot 1−Scentro | Electronegativity difference between top and bottom surface elements, screened by symmetry. |
| Asymmetric radius index | Jr | Jr=rtopvdW−rbotvdWmaxrtopvdW,rbotvdW 1−Scentro | Relative van der Waals radius difference between top and bottom surfaces, screened by symmetry. |

Note. Mcell is the total atomic mass of the unit cell in atomic mass units; 1.660539 is the unit-conversion factor 1 u/Å31 g/cm3; rvdW uses the Bondi consensus radii; and the screening factor 1−Scentro forces the Janus indices of centrosymmetric structures to zero.

Supplementary Fig. S1 | Pearson-correlation analysis of representative descriptors

The Pearson-correlation coefficients quantify linear associations between selected descriptors and the electronic, ionic, and total dielectric responses. Positive values indicate that the descriptor tends to increase with the corresponding dielectric contribution, whereas negative values indicate an inverse trend. The magnitude should be interpreted only as a linear correlation; nonlinear feature effects are discussed in the main text through SHAP analysis.

Supplementary Fig. S1. Grayscale rendering of Pearson-correlation coefficients for representative descriptors associated with (a) the electronic contribution, (b) the ionic contribution, and (c) the total dielectric constant.

| Target response | Descriptor abbreviation | Pearson coefficient |
| --- | --- | --- |
| εelec | Mode Melting T | 0.42 |
| εelec | Max EN Difference | -0.47 |
| εelec | Max EN | -0.50 |
| εelec | Mean Abs Dev EN | -0.46 |
| εelec | OFM:p4-d10 | 0.47 |
| εionic | Covalent Radius Mean Abs Dev | 0.06 |
| εionic | Mean Melting T | -0.09 |
| εionic | Min GS Volume Per Atom | 0.19 |
| εionic | Mean Shell-1 Ordering | 0.24 |
| εionic | RDF 4.9-5.0 A | -0.14 |
| εtotal | Effective Density | 0.31 |
| εtotal | OFM:p4-d10 | 0.36 |
| εtotal | RDF 4.9-5.0 A | -0.19 |
| εtotal | Mean p-unfilled | 0.34 |
| εtotal | OFM:s2-p4 | 0.21 |

Supplementary Table S2 | Feature abbreviations, original feature names, and physical meanings

This table maps the abbreviated descriptors shown in the feature-ranking and distribution figures to their original feature names and physical meanings. The notation follows the naming conventions used by the feature-generation workflow.

| Physical abbreviation | Original feature name | Physical meaning |
| --- | --- | --- |
| Mode Melting T | MagpieData_mode_MeltingT | Mode of the melting points of constituent elements. |
| Max EN Difference | Max_EN_Diff | Maximum electronegativity difference between constituent atoms. |
| Max EN | MagpieData_maximum_Electronegativity | Maximum electronegativity among constituent elements. |
| Mean Abs Dev EN | MagpieData_avg_dev_Electronegativity | Mean absolute deviation of the electronegativity of constituent elements. |
| OFM:p4-d10 | OFM__p_4___d_10 | p4-d10 valence-orbital interaction or co-occurrence component in the orbital field matrix. |
| Covalent Radius Mean Abs Dev | MagpieData_avg_dev_CovalentRadius | Mean absolute deviation of the covalent radius of constituent elements. |
| Mean Melting T | MagpieData_mean_MeltingT | Mean melting point of constituent elements. |
| Min GS Volume Per Atom | MagpieData_minimum_GSvolume_pa | Minimum ground-state atomic volume per atom among constituent elements. |
| Mean Shell-1 Ordering | mean_ordering_parameter_shell_1 | Mean ordering parameter of the first nearest-neighbor shell. |
| RDF 4.9-5.0 A | rdf__4_90000___5_00000_A | Radial distribution function intensity in the 4.9-5.0 A distance range. |
| Effective Density | Effective_Density | Effective density descriptor computed using the effective layer volume rather than the raw supercell volume. |
| Mean p-unfilled | MagpieData_mean_NpUnfilled | Mean number of unfilled p-valence states among constituent elements. |
| OFM:s2-p4 | OFM__s_2___p_4 | s2-p4 valence-orbital interaction or co-occurrence component in the orbital field matrix. |